Todd Miller

Concrete Beam Project

Learning Objectives

Students will:

Concepts:

- Identify the components of concrete, how it is made, and the history and benefits of using it as a building material

- Review the concepts of tension and compression and how they relate to the behavior of concrete beams

- Learn why and how aggregate type and size, and component ratios affects concrete beam behavior.

Scientific Method and Tools:

- Form and test a hypothesis on the failure mode of concrete beams

- Observe the behavior of concrete beams

Communication and Collaboration Skills:

- Work effectively in a small group.

- Present group work effectively to others

- Constructively critique one’s own ideas and those of other learners

- Present their work in an organized and clear manner.